**Typical Surface treatment for JJJ ( made of CCC ) :**

|  |
| --- |
| ****Surface Treatment**** |
| **Hot dip galvanize** |
| Standard : JIS , DIN , ASTM B695 - 2000 |
| Hot dip galvanizing hole cutting good looking on surface |
| Galvanizing process :  Steel structural components → Degreasing → Rinsing→ Pickling → Rinsing →  Fluxing → Galvanizing → Quenching → (Passivation) → Inspecting → Finished Product |
|  |
| **Paint** |
| 1 . Primer paint one coat 20 - 30 um |
| 2 . Middle paint two coat 40 - 60 um |
| 3 . Finish paint one coat 20 - 30 um  Paint type : 1 . red primer  2 . zinc primer  3 . Alkyd primer |